## Slide 1
TTC2022 Aomori, WG-1: Progress of High Q and High Gradient activities
Frequency shift and Q of disordered superconducting RF cavities
PHY-1734332
Department Physics & Astronomy, Louisiana State University, Baton Rouge LA
Hikaru Ueki, Mehdi Zarea, and J. A. Sauls

## Slide 2: Introduction
Niobium superconducting radio-frequency (SRF) cavities are high quality electromagnetic resonators.
Nb SRF cavities with unprecendented quality factors, , have been achieved by infusing Nitrogen into the Nb surface [1-3].
[1] A. Grassellino et al., Supercond. Sci. Technol. 26, 102001 (2013). [2] A. Romanenko et al., Appl. Phys. Lett. 105, 234103 (2014). [3] A. Romanenko et al., Phys. Rev. Applied 13, 034032 (2020).
Mechanism of the improvement has not yet fully understood

## Slide 3: Introduction
These high- cavities provide a new technology platform for both quantum processors, and quantum sensors for axions including dark matter candidates and the Euler-Heisenberg (EH) term of low-energy QED [4-6].
The sensitivity to the axion and EH signals depends on the of SRF cavities.
[4] Z. Bogorad et al., Phys. Rev. Lett. 123, 021801 (2019). [5] Y. Kahn et al., Proc. SPIE 12016, 1201606 (2022). [6] A. Berlin et al., J. High Energ. Phys. 2020, 88 (2020).
Intermodulation due to the nonlinearity in a cavity pumped with two resonance modes
Light-by-light scattering mediated by axion and electrons!

## Slide 4: Introduction
Bafia et al. measured the frequency shift of N-doped Nb SRF cavities near in detail [7].
The high- SRF cavities have “dip” feature in the frequency shift.
[7] D. Bafia et al., arXiv:2103.10601.
Important to study the N impurity effects on the cavity wall

## Slide 5: Introduction
We have developed numerical methods to calculate the quality factor and frequency shift of N-doped Nb SRF cavities based on the quasiclassical theory of superconductivity [8] and the coupling of charge currents to Maxwell’s equations.
We present theoretical results for the electromagnetic response of N-doped Nb SRF cavities as a function of disorder, temperature, and mode frequency.
Our theoretical results are in good agreement with experimental results on both the and frequency shift reported in Ref. [7].
[7] D. Bafia et al., arXiv:2103.10601. [8] D. Rainer and J. A. Sauls, “Superconductivity: From Basic Physics to New Developments”, ch. 2, pp. 45–78, World Scientific, Singapore (1994).

## Slide 6: Formalism
Drude conductivity.
[8] D. Rainer and J. A. Sauls, “Superconductivity: From Basic Physics to New Developments”, ch. 2, pp. 45–78, World Scientific, Singapore (1994).
Conductivity calculated based on the quasiclassical theory of superconductivity: [8]

## Slide 7: Formalism
plasma frequency.
[9] J. C. Slater, Rev. Mod. Phys. 18, 441 (1946).
Surface impedance obtained by solving Maxwell's equations on interface between vacuum and superconductor:
Normal-state resistance , reactance , and conductivity :
Quality factor and frequency shift of the SRF cavities calculated from Maxwell’s equations in a hollow cavity based on the Slater method: [9]

## Slide 8: Theoretical Calculation of Frequency Shift
The green line has the “dip” feature as seen in the high- cavities.
The red and blue lines are the same behavior as the experimental data called the “foot” and “bump” feature, respectively [7].
[7] D. Bafia et al., arXiv:2103.10601.

## Slide 9: Theoretical Calculation of Quality Factor
The quality factor in cavities with intermediate disorder is the largest.
It becomes rather small in the too dirty cavities due to the pair breaking.

## Slide 10: Comparison & Analysis of N-doped Nb SRF Cavities
[7] D. Bafia et al., arXiv:2103.10601.
Bafia et al. measured the frequency shift of Nb SRF cavities near in detail [7].
The weak coupling theory cannot fit well with the peak position and spread in the dip of the frequency shift in the experimental data.
The transition temperature varies depending on where it is measured.
We consider this spread in our calculations.

## Slide 11: Superconducting Gap with Spread in
Gap energy with spread in [11]
Gaussian distribution of [11]
Average of : .
Standard deviation of : .
and are fitting parameters
[11] HU, M. Zarea, and J. A. Sauls, arXiv:2207.14236.

## Slide 12: Spread in and Inhomogeneity of Impurities
[12] M. Zarea, HU, and J. A. Sauls, arXiv:2201.07403.
equation:
Transition temperature for pure Nb: K.
Gap anisotropy factor: .
These parameters are obtained from the LDA calculation [12].
This spread comes from inhomogeneity of impurities.

## Slide 13: Comparison & Analysis of N-doped Nb SRF Cavities
Frequency shift of the N-doped Nb SRF cavities with the different frequency: [7]
[7] D. Bafia et al., arXiv:2103.10601.
Our theoretical lines are fitted well with the experimental data!

## Slide 14: Comparison & Analysis of N-doped Nb SRF Cavities
Gap energy near and Gaussian distributions of and :
Used , , , and the corresponding experimental data: [7]
[7] D. Bafia et al., arXiv:2103.10601.
Our theory is in good agreement with the experimental data!

## Slide 15: Comparison & Analysis of N-doped Nb SRF Cavities
Quality factor and frequency shift of the Nb SRF cavity: [7]
[7] D. Bafia et al., arXiv:2103.10601.
The calculation of is not perfect but in reasonable agreement with the experimental data.

## Slide 16: Summary
We showed that the quality factor has a peak of upper convexity as a function of the quasiparticle-impurity scattering rate, with the largest 𝑄 in cavities with intermediate disorder.
We presented theoretical results for the effects of inhomogeneous disorder on the transition temperature and frequency shift of SRF cavities and our calculations are in good agreement with the experimental results [7].
We provide a new tool for characterization of high-𝑄 SRF cavities.
We thank D. Bafia, A. Grassellino, A. Romanenko, and J. Zasadzinski for many discussions on their experimental work on SRF cavities.
[7] D. Bafia et al., arXiv:2103.10601.

## Slide 17: Main Message
The quality factor has a peak of upper convexity as a function of the impurity scattering rate, with the largest 𝑄 in cavities with intermediate disorder.
The effects of inhomogeneous disorder on are very important for the frequency shift of the SRF cavities near .
Taking Points
Why is Q the largest at intermediate levels of disorder?
Why do the Nb SRF cavities with intermediate levels of disorder have the dip feature in the frequency shift?

## Slide 19: Comparison & Analysis of a Nb Sample in a Cooper Cavity
Frequency shift and quality factor of a Nb sample in a cooper cavity: [10]
[10] O. Klein et al., Phys. Rev. B 50, 6307 (1994).
The comparison for is not perfect, but the experimental data does have significant scatter. That for is much better.

## Slide 20: Frequency Shift Anomaly Near
[11] HU, M. Zarea, and J. A. Sauls, arXiv:2207.14236.
To understand the dip in the frequency shift, we express the conductivity as [11]
and are the small deviations from and , respectively.
Assuming , we obtain the frequency shift near as
is now satisfied since is larger in dirty superconductors, and then the frequency shift becomes negative near .