## Slide 1
Hannah Hu, Daniel Bafia, Young-Kee Kim
TTC 2022, Aomori, Japan
11 October 2022
Development of Oxygen Doping Treatment for High Q0

## Slide 2: Motivation
Superconducting radiofrequency (SRF) cavities
  High quality factors (Q0)
  High accelerating gradients (Eacc)
Performance is largely governed by the first ~100 nm (rf layer)
Baking and chemical treatments alter the composition of the rf layer
Nitrogen doping
Tailoring of the impurity profile via oxygen doping
O doping and N doping yield similar performance.
What precise roles are O and N and playing?

## Slide 3: Nitrogen Doping vs Oxygen Doping
N Doping 2/0 + 5 um
Baked in UHV furnace at 800 C injection of 25 mTorr for 2 minutes
5 um EP removal
O Doping
Baked in-situ at 200 C for 20 hours
  Maintains Torr
  Utilizes thermal diffusion without any subsequent chemistry
Both yield uniform concentration of impurities within the rf layer.
°
°
O/Nb SIMS: A. Romanenko et al., THP014, SRF’19 (2019).
NbN SIMS: D. Bafia. PhD Thesis, IIT, 2020

## Slide 4: Cavity Treatment
Single cell, tesla shaped Nb cavities
1.3 GHz resonant frequency
Continuous wave (CW) operation
Treatment
200°C x 20 hrs
HF Rinse 1
HF Rinse 2
N doped
HF Rinse: A. Romanenko et al., Phys. Rev. ST Accel. Beams 16 (2013).

## Slide 5: Quality Factor (Q0) vs Accelerating Gradient (Eacc)
N Doping
High Q0 > 4
Eacc < 38 MV/m
O Doping
High Q0 ~ 4.3
Eacc ~ 33 MV/m
Multipacting induced quench which
trapped flux

## Slide 6: Anti-Q Slope and BCS Resistance
Anti-Q slope phenomenon
Decrease in RBCS with field
RBCS is not affected by HF rinse changing the oxide → impurity profile is mostly unchanged
Compared to N doped: High field losses

## Slide 7: Residual Resistance Rres
Moderately low
Increase in Rres from partially refreshed oxide
Decrease in Rres with fully refreshed oxide
Regrowing native oxide mitigated some sources of loss
Growth of suboxides from in-situ baking treatment may have driven lower Q0
Compared to N doped: increased at high fields
Drives difference in Q0

## Slide 8: TMAP
N doped 2/0 + 5
N doped TMAP: D. Bafia, PhD Thesis, IIT, 2020
O doped + 2 HF Rinses TMAP at low T (~1.5 K) taken just before quench (~33 MV/m)
Quench Location

## Slide 9: Heating Profile
Change in temperature at quench location with peak magnetic field
Pure Joule heating – slope of 2 according to Ohm’s law
O doped: Turning on of additional loss mechanisms at higher fields
Might be one reason why resistance in O doped is much stronger compared to N doped
slope: 2.18
slope: 9.36
slope: 4.49
N doped
O doped

## Slide 10: Anomalous Dip in Resonant Frequency Before Tc
Tc
 | Tc [K]
N doped | 9.42
O doped | 9.34
+HF Rinse 1 | 9.36
+HF Rinse 2 | 9.36
Tc suppression in oxygen doped cavity: weakened superconductivity may be source of high field losses

## Slide 11: Anomalous Dip in Resonant Frequency Before Tc
 | Δ fdip [kHz]
N doped | 1.31
O doped | 0.54
+HF Rinse 1 | 0.26
+HF Rinse 2 | 0.25
Δ fdip
Two types of dip behavior:
  O doped: “dip+bump” characteristic behavior observed in some N infused cavities
  O doped + HF rinse: “dip” feature observed in N doped cavities
Magnitude of “bump” = Magnitude of “dip” after HF rinse
  2nd HF rinse has no additional effect
Could this be a double effect?
Two localized effects: different Nb2O5/Nb interface → different dip behavior
Larger dip from the suboxide interface
  Eliminated when oxide is refreshed
Smaller dip from the interstitial oxygen that thermally diffused

## Slide 12: Summary
Oxygen and nitrogen doping yield similar rf performance
Performance of oxygen doped cavities limited by high field losses generating substantial heating
Tc suppression in oxygen doped cavity: weakened superconductivity may be source of high field losses
Both O and N doped cavities display frequency dip before Tc
  O doped shows a localized double effect in dip features
Tailor oxygen doping impurity profile to match nitrogen doping impurity profile
Exploring sources of loss mechanisms that turn on at higher fields
Next Steps

## Slide 13
Thank you!

## Slide 14
Supplemental Slides

## Slide 15: Superconducting gap Δ, mean free path
 | Δ [meV] | mfp [nm]
N doped | 2.10 ± 0.08 | 125.1 ± 37.8
O doped | 2.18 ± 0.04 | 17.99 ± 1.12
+HF Rinse 1 | 1.69 ± 0.02 | 14.52 ± 0.56
+HF Rinse 2 | 1.98 ± 0.03 | 16.79 ± 0.79
Comparable average superconducting gap Δ
  Oxygen doping reduces QP introduced losses
Smaller mfp: higher concentration of impurities on the surface of an oxygen doped cavity
  Confirmed with SIMS
  Effects of tailoring oxygen doping treatment to have same mfp as nitrogen doping?
D. Bafia, PhD Thesis, IIT, 2020