## Slide 1: Dynamic flux trapping measurements in Nb samples
TTC Meeting in Aomori, Japan, 10.10. – 14.10.2022
TTC
Aomori, Japan
F. Kramer, S. Keckert, O. Kugeler, J. Knobloch

## Slide 2: Brief recap: Why do we care about trapped flux?
Trapped flux reduces Q0 in SRF cavities
Trapped flux is currently believed to be the predominant limitation for Q0
Double magnetic shielding reduces ambient Earth magnetic field from 50 µT to < 1 µT
But it is impossible to completely shield off all magnetic fields
Shielding does not reduce intrinsic fields caused by thermo currents
Introduction
10 µT
ambient Earth magnetic field = 50 µT

## Slide 3: Trapped Flux: What is it?
When cooling down a Type I superconductor in an external magnetic field, it will transition into the Meissner state. In this state all magnetic field is expelled.
However, there are small defects in the material which pin the quantized magnetic field lines and prevent them from being pushed out
The pinned flux lines oscillate in the RF field and cause losses in the cavity wall*
Introduction
NC
Field
SC
Field
SC
No Field
Ideal
Not ideal
*Gurevich, A. and Ciovati, G., Effect of vortex hotspots on the radio-frequency surface resistance, Phys. Rev. B, 2013

## Slide 4: Concept – revert to flat samples
We want to understand trapped flux in more detail, before trying to minimize it
To understand trapped flux, we need control parameters which might have an influence on it:
  Temperature gradient
  Cooldown speed
  Ambient magnetic field
  Impact of geometry (demagnetization factor, shape anisotropy)
  Material & treatment
Experiment
Use samples instead of cavities
Better Control of the parameters
More cooling cycles possible (~300/day instead of ~1/day)
Less material needed and treatments are easier to apply
Easier geometry
60 mm
100 mm
Investigate Nb sheets
~300 cycles per day
AMR based magnetometry system developed
at HZB for cavities in 2017 – 1 cycle per day

## Slide 5: Experimental Infrastructure
Small glass cryostat
Filled from helium Dewar
No magnetic shielding
Active field compensation with two Helmholtz coils and one solenoid
Minimum field at location of reference sensors: < 15 nT (Earth magnetic field ~ 50 µT)
Maximum field: 200µT
Experiment

## Slide 6: Experimental setup
Sample (100x60x3)mm, clamped in copper blocks at either end
Setup is suspended above liquid helium bath
Heater in helium is used to control helium gas flow
Dual heaters on the end of the blocks allow for precise control of temperature gradient and cooldown speed
Blocks move electric heaters away from sample, this reduces magnetic fields from the heaters at the sample
8 Cernox sensors measure temperature distribution across sample
Multiple AMR sensors for magnetic field measurements
grouping of 3 sensors to measure field vector in 3d
15 AMR sensor groups measure magnetic field just above the sample
Experiment
Heater
LHe
Cernox
Nb
Cu blocks
Heater
PCB with AMR sensors

## Slide 7: A typical Cooldown
Apply external field Bext = 100 µT
Set Temperature gradient across sample (∇T = 0.06 K/cm)
Lower Sample temperature at top and bottom simultaneously
After Sample is fully superconducting, remove external field Bext = 0 µT
Measure trapped flux
Results
9.5K
10.1 K
8.9K
9.5K
nc
sc

## Slide 8: Trapped flux vs Temperature Gradient
Vary temperature gradient while keeping external magnetic field and cooldown speed constant
  Bext = 100 µT
  dT/dt = 0.07 K/s
Comparison between fine grain sample and large grain sample (both untreated)
Less trapped flux with higher temperature gradient
Large grain material allows near 100% flux expulsion
Data disagrees with model proposed by Kubo*
  Reason might be a too high field level
Results
Large Grain
Fine Grain
100% trapping
Kubo Model
* Kubo, T., Flux trapping in superconducting accelerating cavities during cooling down with a spatial temperature gradient, Prog. Theor. Exp. Phys., 2016

## Slide 9: Trapped Flux Vs ambient Field
Vary magnetic field strength with constant temperature gradient and cooldown speed
Change Temperature gradient for different measurement runs
  Large grain sample
  dT/dt = 0.07 K/s
  ∇T = 0 K/cm; 0.04 K/cm; 0.1 K/cm
Flux is not trapped below a gradient-dependent threshold field
Above threshold the dependence is linear
Slope decreases with increasing temperature gradient
This threshold behavior is not observed in fine grain sample
Results
Increasing ∇T
Large grain Nb sample

## Slide 10: Trapped Flux vs Cooldown Speed
Vary cooldown speed while keeping temperature gradient and external magnetic field constant
Alter temperature gradient for different measurement series
  Large grain sample
  Bext = 100 µT
  ∇T = 0.04 K/cm; 0.07 K/cm; 0.1 K/cm
Increasing Trapped Flux with decreasing Transition Time
No difference after ~10s
Results

## Slide 11: Conclusion
Temperature Gradient / Material
Better expulsion at higher gradients
Large grain expels flux much more efficiently than fine grain
Above 0.1 K/cm all flux is expelled in large grain sample
External magnetic field
Depending on temperature gradient, flux is only trapped above threshold field
Linear dependency above threshold field
Cooldown speed
Flux needs time to exit the superconductor
Conclusion & Outlook
Outlook
Develop a model combining the results obtained so far
Investigate different Materials (coated Nb, Nb3Sn, multilayer)
  Nb on Cu currently under investigation
Investigate how different material treatments influence trapped flux
Develop methods to decrease trapped flux