## Slide 1: Nb3Sn cavity coating development for accelerator applications at Jefferson Lab
Uttar Pudasaini
Notes: Nb3Sn

## Slide 2: Acknowledgements
Jefferson Lab
  Charlie Reece
  Anne-Marie Valente
  Bob Rimmer
  Tony Reiley
  Michael Kelley
  Gianluigi Ciovati‬
  John Vennekate
  SRF Technical staffs
Old Dominion University
  Jayendrika Tiskumara
Fermilab
  Grigory Eremeev

## Slide 3: Outline
Vapor Diffusion Coating
Cavity coating
  Single-cell Cavity Coating
  Five-cell Cavity Coating
Cavities for conduction-cooled Accelerator Applications

## Slide 4: Vapor Diffusion Coating of Nb3Sn on Nb
Leading coating technique to produce promising cavities
Create Sn-vapor, transfer to the interior surface of Nb cavity
Growth at Nb-Nb3Sn interface
2-3 µm thick
Cross-section
Cross-section

## Slide 5: Performance of Single-cell cavity
Known limitations:
Non-uniform coating – forming patchy region
Potential Ti-contamination
Sn residues by condensation of Sn vapor
~85 °C
Potential limitations:
Non-uniform coating – forming patchy region
Potential Ti-contamination
Mitigation Sn residues
Pudasaini U, Eremeev G, Reece CE, Ciovati G, Parajuli I, Sayeed N, Kelley MJ. Recent results from Nb3Sn single cell cavities coated at Jefferson lab. InProc. 19th International Conference on RF Superconductivity,(SRF’19) 2019 Jun.

## Slide 6: Evolution of coating temperature profile and cavity performance
Ra = 53 ± 4 nm
Ra = 123 ± 13 nm
Single-cavity Setup
Vary Sn-source and/or Temp profile or set up
Pull plug to relieve Sn-vapor

## Slide 7: Toward higher gradients
Secondary Sn source with conical crucibles
1.5 GHz cavity

## Slide 8: Recent performance of single-cell cavity
No quench, limited by input power
Exhausted Sn source
With Sn-residues (Typical Q-slope)
The coating profile update was guided by the witness sample analysis.
The coating profile currently followed aims to obtain equivalent coating grown at 1200 °C for ~ 1 h.
Notes: Q-slope

## Slide 9: RF performance compared with material analysis
TEM analysis of grain boundaries with and without Q-slope
Coating with small grain sizes, smoother surfaces, and thinner coating avoiding annealing without Sn correlates with better performing cavities.
Q-slope
Annealed
No No Q-slope
Performance | Typical – Q slope | “Good” | Annealed – “bad”
Average grain size (µm) | 1.52 ± 0.19 | 0.96 ± 0.06 | 1.11 ± 0.08
Average roughness (nm), 50 um scan | 202 ± 54 | 73±8 | 98 ± 5
Average thickness (µm) | 2.06 ± 0.49 | 1.20 ± 0.12 | 1.75 ± 0.15
GB composition |  |  | Sn-deficient
No Sn-rich GBs.
Sample with annealing features – Sn deficient GBs.
No obvious compositional difference between single-step (thicker) coating and three-step (thinner coating): generous Sn flux?
Sn-deficient regions were observed close to the Nb3Sn-Nb interface.
Do Q-slope is related to thickness and roughness?
Smoother, thinner, uniform coating??
Annealed without Sn
1200C × 3 h
Notes: Q-slope

## Slide 10: Management of Sn supply
Changing Sn effusion area for fixed substrate area:
  Larger crucible - higher evaporation - larger grain size and rougher surface.
  Small crucible - insufficient Sn-supply - non-uniform coating like observed during the coating of a larger or longer cavity coating
Changing substrate area for fixed Sn effusion area
  Increasing Substrate surface area - higher Sn-evaporation -microstructure and roughness defined by the Sn supply to the substrate area.
Area of both substrate and source need careful attention during the process design to engineer desired surface properties of the film.
Sn-flux (substrate size, source size, and temperature) at the initial stage and coating stage is crucial.
U. Pudasaini, C. E. Reece, and J. K. Tiskumara, “Managing Sn-Supply to Tune Surface Characteristics of Vapor-Diffusion Coating of Nb3Sn”, presented at the SRF'21, East Lansing, MI, USA, Jun.-Jul. 2021, paper TUPTEV013, unpublished. doi:10.18429/JACoW-SRF2021-TUPTEV013 C

## Slide 11: Surface roughness reduction
Scan size 20µm ×20 µm (Averaged from two randomly selected areas) | NX07 | CW36 | CW44
Rq (nm) | 104.5 ± 3.5 | 86 ± 2 | 51 ± 1
Ra (nm) | 83.4 ± 3.1 | 69 ± 3 | 40 ± 1
Uniform coating
Sn residues are eliminated or significantly reduced
Thickness needs to be measured.
More experiments are underway.
Cavity coating is planned for RF analysis.
NX07
CW36
CW44

## Slide 12
CEBAF Five-cell cavity coating

## Slide 13: Process design: setup and temperature profiles
Sn consumption (g) |  |  |  |  | 
 | IA163 (1st coating) | IA163 (2nd Coating) | IA163 (3rd Coating) | 5C75-RI-NbSn02 02 | 5C75-RI-NbSn02 02
Primary | 3.6 | 2.50 | 2.79 | 3.05 | 2.42
Secondary 1 | 1.7 | 1.50 | 1.42 | 1.50 | 1.48
Secondary 2 | --- | 1.60 | 1.43 | 1.51 | 1.48
Total | 5.3 | 5.60 | 5.64 | 6.06 | 5. 38
Setup | S1-T1 | S2-T1 | S3-T2 | S2-T1 | S3-T2
S1
S2
S3
T1 T2
Witness samples in each run.

## Slide 14: Latest CEBAF Five-cell C75 cavity coating
The Cavity was coated for a Nb3Sn cavity pair to install in a quarter cryomodule (built on Grigory Eremeev’s ECA).
C75 cavity made from large grain Nb.
Temperature Profile
S3-T2

## Slide 15: Nb3Sn pair assembly (Second time)
At 4K : Q~1E10 @ >10 MV/m
Limited by multipacting at 13.5 MV/m: no attempt to process it.
Coated and qualified at Fermilab (G. Eremeev)
Coated and qualified at Jefferson Lab
The goal is to install the QCM and test in JLab UITF (beam test.)
- More details on tomorrow’s talk “Progress in Nb3Sn developments for CEBAF-style quarter cryomodule​”.

## Slide 16: -
Cavity Coating for Conduction cooling Accelerator Applications

## Slide 17: 952 MHz Prototype cavity
Coated for the second time with added Sn-source (3 Sn sources)
After copper plating with ring for conduction cooling, tested with LHe.
Test in a horizontal cryostat at industrial partner, General Atomics, very soon.
More on G. Cheng’s talk “952MHz Nb3Sn Cryostat Design and Thermal Management” tomorrow.
PI: Gianluigi Ciovati
J. Vennekate et. al. LInac 2022
Notes: Multipacting

## Slide 18: Design and Prototyping for a Compact 10 MeV SRF Accelerator
• Cavity is baselined
(Q >1E10 @ ~ 18 MV/m)
• HW required for the coating is in progress.
• Cavity coating projected to January 2023.
• Collaboration with General Atomics.
PI: John Vennekate
1.3 GHz TESLA 3-cell cavity
J. Vennekate et. al. LInac 2022

## Slide 19: Summary
The optimization of coating parameters is ongoing to engineer desired surfaces that may enhance single-cell and multi-cell cavity performance.
A generous tin flux is required at the initial stage to grow the coating uniformly.
  Crucible size, substrate surface area, and temperature needs proper management
It is crucial to make sure not to run the coating up to complete Sn exhaustion resulting in Sn-deficient grain boundaries or even loss of Sn from the surface.
Proper management of Sn-supply can result in smoother and uniform surface, which appears to correlate with better performing cavities.
Recurrent Sn condensation is mitigated with the latest parameters, but complete removal is challenging with our coating configuration.
Single-cell and five-cell Nb3Sn-coated cavities are heading towards other acceleration applications, including conduction cooling.

## Slide 21: Backup slides

## Slide 22
Proposed for ERL application in the past
Twin axis cavities were coated and tested.
Mechanical deformation of the cavity
Following witness sample analysis, systematic sample studies are in progress to mitigate identified issues.
Nb3Sn coating of Twin-axis Cavity
Prof. Jean Delayen and Jayendrika Tiskumara (Old Dominion University)

## Slide 23: Nb3Sn Coating deposition system
40’’
17’’
Eremeev, G., et al. "Nb3Sn multicell cavity coating system at Jefferson Lab." Review of Scientific Instruments 91.7 (2020): 073911.
Coating up to the size of CEBAF five-cell cavity (0.5 m long)
Siemens Configuration: No secondary heater(s) (substrate and source both at the same temperature for any time)
Furnace is outside the cleanroom: Need to close the cavity to avoid contamination